# JCOMA-25-4218 Revision 1 — Questions for the FEM Co-author

We need precise numeric / methodological answers to address several reviewer comments on the FE model (Section 2.2) and the material card (Table 1). Six items, one short reply per question is sufficient.

# Q1 — Cohesive interface stiffness (Reviewer 2)

Table 1 currently lists:

| Parameter | Value as printed |
| --- | --- |
| Normal stiffness K_nn | 100 N/mm³ |
| Shear stiffness K_ss = K_tt | 35 N/mm³ |

Reviewer 2 argues these are three orders of magnitude too low — they should be 100 kN/mm³ and 35 kN/mm³ (≈ 10⁵ N/mm³, the physically realistic penalty stiffness for a toughened-epoxy adhesive).

What value was actually used in the Abaqus .inp file? A single-line answer is fine (e.g., "100 000 N/mm³" or "100 N/mm³ — chosen as a soft penalty stiffness for a specific reason").

# Q2 — Cohesive fracture energies (Reviewer 2)

Table 1 lists G_Ic = 400 J/m² and G_IIc = 600 J/m². The lamina fracture energies are in N/mm. Reviewer 2 asks for unit consistency. The straight conversion gives:

400 J/m² = 0.4 N/mm

600 J/m² = 0.6 N/mm

Are these the values that were in the .inp file? Confirm or correct.

# Q3 — Through-thickness ply discretisation (Reviewer 1)

Reviewer 1: "Were the layers modelled explicitly in the base laminate and the repaired part?"

The current text in §2.2 says SC8R elements were used, plus a passing mention of a "sub-laminate approach". That's ambiguous. Please confirm which of the following matches the actual model:

(a) One SC8R element per ply — 9 elements through the parent (layup [45/-45/90/0/90/0/90/-45/45]) and 6 elements through the patch (layup [0/90/0/90/-45/45]).

(b) Sub-laminate stacks — plies grouped into N stacks, each stack one SC8R element with a composite section. If so, what was the grouping?

(c) A single SC8R element through-thickness with a composite section integrating the full layup analytically.

# Q4 — Material identification (Reviewer 1)

Reviewer 1: "Graphite/Epoxy UD IMS 24K 977-2 — there is not enough data to identify the material. Which IMS fibres? Is 977-2 an epoxy resin? State the manufacturer."

Best guess from the literature: Toho Tenax IMS65 24K carbon fibres impregnated with Solvay/Cytec CYCOM 977-2 toughened epoxy resin, supplied as a unidirectional prepreg by Solvay. Please confirm — and correct any of the three pieces below:

Fibre grade & manufacturer (e.g., Tenax IMS65 24K, Toho Tenax / Teijin Carbon)

Resin grade & manufacturer (e.g., CYCOM 977-2, Solvay)

Prepreg supplier / part number (e.g., Solvay CYCOM 977-2 UD prepreg)

# Q5 — Mesh convergence study (Reviewer 2 — Step #9 ahead)

Reviewer 2 raises the concern that the ~95 % strength-recovery limit may be mesh-dependent, because stress concentrations at the step corners are sensitive to element size. To answer this:

Was a mesh convergence study performed? (The paper currently only says the cohesive zone length L_cz is spanned by 3–5 elements.)

If yes: what element sizes were tested, and at what density was the result considered converged?

Was the ~95 % saturation reproduced across multiple meshes (i.e., is the asymptote a stable feature, or could a finer mesh push it higher / lower)?

# Q6 — Anything else

Is there any other FE or material detail that should appear in §2.2 or Table 1 to make the model fully reproducible for a peer reviewer? (e.g., damage-evolution law type, BK exponent η for mixed-mode, viscous regularisation, etc.)

Please reply inline under each question; one or two lines per item is plenty. I'll then incorporate the answers into the revised manuscript and Table 1.